## Slide 1
APPLICATION OF DIFFERENT MATERIALS IN BONE IMPLANTOLOGY
BRUNO KÖNIG JÚNIOR
SÉRGIO ALLEGRINI JUNIOR

## Slide 2
SIX KINDS OF CALCIUM PHOSPHATE CERAMICS WERE INSTALLED IN THE RABBIT’S TIBIAE: CaHPO4, Ca(HPO4)2H2O, Ca2P2O7, Ca3(PO4)2 Ca9(PO4)6(OH)2, and Ca10 (PO4)6(OH)2, .
The fluorescense microscopy was used in order to observe the periodic osteoconduction/deposition properties of the different ceramics of calcium phosphate. The animals were subcutaneously injected with fluorescent apatite labeling chemicals.
Alizarin was injected in the 2nd and 3rd , calcein in the 4th and 5th and tetracycline in the 6th and 7th postoperative weeks. Sacrifice took place in the 8th week.
The technique used for calcified tissue histologic preparation is the one developed by Karl Donath from the Hamburg University (Donath, K. Die Trenn-Dünnschliff-Technik zur Herstellung histologischer Präparate von schneidbaren Geweben und Materialen. Der Präparator, 34: 197-206, 1988).

## Slide 3
CaHPO4 (Dicalcium anhydrid phosphate) – Photomontage of a rabbit’s tibia transverse section in fluorescence microscopy. The fluorescent labels Alizarine (2nd and 3rd weeks after surgery – brick red in color), Calcein (4th and 5th weeks after surgery – yellow green in color) and Tetracycline (6th and 7th weeks after surgery – orange in color) indicate different periods of calcium deposition. 10X in the microscope.
KÖNIG & RESEARCH TEAM
GRAFT

## Slide 4
B
Ost
Fluorescent photomicrograph of a titanium implant covered with anhydrid phosphate calcium ceramic (CaHPO4) showing different periods of calcification enhanced by different colors. Great activity in the alizarin and calcein periods. B = mature bone, Ost = Osteon, A = Alizarin, C = Calcein, T = A tetracycline osteonic ring and Cr = Ceramic . 100X in the original.
KÖNIG & MITRI
TITANIUM
IMPLANT
Cr
A
T
C
Cr

## Slide 5
Fluorescent micrograph with a titanium implant covered with a dicalcium dihydrated
ceramic (CaHPO42H2O) showing different periods of calcification enhanced by different
colors. There is a great amount of newly formed bone tissue. A = Alizarin; C = calcein;
T = Tetracycline and Cr = Ceramic. Less calcification was observed in the alizarin period,
that is in the beginning of the deposition process. 100X in the microscope.
TITANIUM
IMPLANT
T
A
C
Cr
KÖNIG & MITRI

## Slide 6
Osteoconduction results of titanium implants coated with pyrophosphate calcium ceramic - Ca2P2O7.
A - Photomicrography of the control group under fluorescent light. The thread of the implant screw is fulfilled with concentric or parallel lamellar bone with a predominance of calcein labeling. (Ca = calcein, Os = osteon), bar = 150 m.
B – Photomicrograph of the experimental group under fluorescent light. A predominance of calcein labeling, but with a lesser amount, is to be seen. (Ca=calcein, Os = osteon), bar = 150 m.
A
B
TITANIUM
IMPLANT
TITANIUM
IMPLANT
KÖNIG & KOO

## Slide 7
CONTROL GROUP
EXPERIMENTAL GROUP
Ca2P2O7
KÖNIG & KOO

## Slide 8
Three phases of fluorescence of calcification periods in a dental alveolar cavity after tooth extraction grafted with reabsorbable Hydroxyapatite (HA) Ca9(PO4)6(OH)2 30X in the original.
Image of fluorescence microscopy of a dental alveolar cavity after tooth extraction grafted with not absorbable HA Ca10(PO4)2(OH)2. A few mineral depositions are to be seen among ceramic crystalloids. 30X in the original.
KÖNIG & DE MELO

## Slide 9
Ca3(PO4)2- Photomontage of a transverse section in fluorescent microscopy of rabbit tibia. Great repair activity areas with bone cortical tissue neoformation (bone remodeling) in the graft insertion area. There are still many granules of the ceramic to be seen after 8 weeks of post operatory time, in the bone marrow region. Layers of bone deposition in the endostal region.10X in the microscope.
KÖNIG & RESEARCH TEAM

## Slide 10
CERAMIC BONE DEPOSITION AREA (IN µm2 ) % CLASSIFICATION |  |  | 
Ca HPO4 | 152.108,00 | 12,18 | 5TH
Ca(HPO4)2H2O | 162.919,54 | 13,04 | 4TH
Ca2P2O7 | 228.813,85 | 18,32 | 3TH
Ca3(PO4)2 | 278.370,96 | 22,28 | 2ND
Ca9(PO4)6(OH)2 | 99.295,03 | 7,95 | 6TH
Ca10(PO4)6(OH)2 | 327.760,07 | 26,24 | 1ST
TOTAL | 1.249.267,45 |  | 

## Slide 11
USE OF BIOACTIVE GLASSES COMPOSED OF PHOSPHATES CONTAINING CALCIUM, SODIUM AND NIOBIUM. MARCELO J. CARBONARI.
Fluorescent micrograph of a bone remodeling and conduction area. Labeling is present – tetracycline (T), alizarin (A) and calcein (C). Osteons (OS) and lamellar parallel bone tissue (LT).
CARBONARI, MARTINELLI & KÖNIG
IMPLANT
T
A
C
C
OS
LT

## Slide 12
BIOCOMPATIBILITY OF SILICON NITRIDE IMPLANTS – Cecilia Chaves Guedes e Silva
1
2
3
Samples of silicon nitride: 1) initial form; 2) after correction and 3) samples to be used “in vivo” testing.
GUEDES E SILVA, BRESSIANI & KÖNIG

## Slide 13
Deflection of a split among pellets of -Si3N4 (arrow).
GUEDES E SILVA, BRESSIANI & KÖNIG

## Slide 14
The Si3N4 ceramic shows itself biocompatible and osteoconductive.
OS – OSTEON
A – ALIZARIN
C – CALCEIN
T – TETRACYCLINE
I - IMPLANT

## Slide 15
Osteointegration of the Ti-13Nb-13Zr alloy to be used as a biomaterial.
Sandra J. Schneider
SCANNING ELECTRON MICROGRAPHIE OT THE ALLOY.
SCHNEIDER, BRESSIANI & KÖNIG

## Slide 16
MATURE BONE
ISLANDS OFBONE
REMODELING
OSTEOCONDUCTION
OF NEWLY FORMED
BONE
PERIOST
Ti-13Nb-13Zr
IMPLANT
FLUORESCENT MICROGRAPH SHOWING THE BIOINTEGRATION OF THE IMPLANT. SCHNEIDER, BRESSIANI & KÖNIG

## Slide 17
Osteointegration of the Ti-13Nb-13Zr alloy obtained by powder metallurgy.
Marco Cícero Martins Bottino.
*
*
Scanning electron microscopy of an Endopore Implant (Innova Corporation, Toronto, ON, Canada), as example: Different magnifications to show porosity.

## Slide 18
Micrographies, obtained by SEM, of the Ti-13Nb-13Zr alloy samples in different magnifications. Clear regions are not diluted Nb particles. Interconnections of the alloy pores. In the color slides it is to see that osteointegration and osteoconduction were achieved. BOTTINO, BRESSIANI & KÖNIG
I
I